## Slide 1: Toward Scalable, High-Fidelity Trapped-Ion Quantum Information Processing
P.I.s: John Chiaverini and Jeremy Sage
QCPR
2 August 2018
This work is sponsored by the Department of Defense under Air Force Contract #FA8721-05-C-0002. Opinions, interpretations, conclusions, and recommendations are those of the author and are not necessarily endorsed by the United States Government.

## Slide 2: Introduction and Outline
Dual-Ion-Species Control
  Goal: Use two ion species for scalable transport and readout; work toward high-fidelity gates with photonics
    Two-qubit MS gates (same species, inter-species)
    Two-ion gate in three-ion chain
Anomalous Heating Studies
  Goal: understand and mitigate ion heating to improve speed / fidelity of quantum logic operations
    Ion-electrode distance dependence
    Ex situ milling of Au and Nb traps as a function of T
Integrated Photonics Development
  Goal: develop scalable platform for integrated photonic control over wide wavelength range
    Visible platform: Al2O3/PECVD SiN (low loss, multi-layer, CMOS-compatible)
    Toward High-efficiency photonic I/O

## Slide 3: Introduction and Outline
Dual-Ion-Species Control
  Goal: Use two ion species for scalable transport and readout; work toward high-fidelity gates with photonics
    Two-qubit MS gates (same species, inter-species)
    Two-ion gate in three-ion chain
Anomalous Heating Studies
  Goal: understand and mitigate ion heating to improve speed / fidelity of quantum logic operations
    Ion-electrode distance dependence
    Ex situ milling of Au and Nb traps as a function of T
Integrated Photonics Development
  Goal: develop scalable platform for integrated photonic control over wide wavelength range
    Visible platform: Al2O3/PECVD SiN (low loss, multi-layer, CMOS-compatible)
    Toward High-efficiency photonic I/O

## Slide 4: Self-Shielding Superconducting Ring Geometry
1.5 mm
7mm
11 mm
Radiation shield
Trap
chip
Lower
niobium ring
Upper
niobium ring
Fluorescence collection window
Laser
window
Applied bias
B-field
Ion
Fluctuations in magnetic field at ion location lead to detuning errors and reduced two-qubit gate fidelity
  Magnetic field can be passively stabilized by installing two co-axial superconducting rings
  Flux conservation through rings induces supercurrents that cancel fluctuating fields
  Superconducting temperature of niobium (Tc = 9.2 K) is higher than our operating temperature (T = 4-5 K) → Superconductivity comes for free
  Low-frequency field fluctuation has been reduced to 30 µG (rms) for a 5 G bias field
c.f. Gabrielse et al. (JMR 1991) and Wang et al. (PRA 2010)

## Slide 5: Improvements to Laser-Ion Coherence
Vibration of cryocooler causes laser phase noise at ion location
  Operating above LHe boiling point reduces coupling of cooler to ion trap, increasing coherence time
  Residual vibrations still have significant negative effect, cf. “Cryocooler off” data point
Integrated photonic grating couplers should further improve coherence time
  Vibration-induced motion of laser and ion becomes common mode
  Measurements using two different transitions show B-field fluctuations do not limit our system coherence at this level
5K to cryocooler off
4K to 5K
k

## Slide 6: Multi-Qubit Chains and Gates: Same Species 2-Qubit Gate
Mølmer – Sørensen Gate
Ca+
Ca+
Two qubit gate fidelity: 98.8%

## Slide 7: Improved Gate Performance in Two Different Atomic Species
Following improvement to lab control systems, two-qubit gate fidelity improved to F = 0.988(2) in Ca+-Ca+
  Control refinements should improved Sr+ gate performance
    F=0.974(2) in Sr+-Sr+
    Extra uncompensated fiber length in Sr+ setup
    Potentially broader laser for Sr+
Improved Sr+ - Sr+ MS gate
Improved Ca+ - Ca+ MS gate

## Slide 8: Inter-Species Entanglement Generation
  This is the first demonstration of an inter-species Mølmer-Sørensen gate using two different optical qubit species (F=0.94)
This same interaction can be used to generate entanglement between ions of different species
  High-fidelity inter-species gate requires high-fidelity operations for both individual species
  Some common-mode rejection is lost
Sr+
Ca+
Ca+ - Sr+ MS gate
c.f. NIST Be+-Mg+, F~0.97 (Nature 2015) and UMD Ba+-Yb+, F=0.60 (PRL 2017)

## Slide 9: Multi-Qubit Chains and Gates: Mixed Species Unit Cell Chain
Dual-cell physical architecture concept
Longer multi-species ion chains can serve as the basis of a scalable QIP architecture
  E.g., surface code error correction
Sr+
Sr+
Ca+

## Slide 10: Logic Gates in Longer Ion Chains
Sr+
Sr+
Ca+
High-fidelity two-qubit operations between ions of the same species
Auxiliary ion of different species used for sympathetic cooling, low-crosstalk state-readout
Recently demonstrated with fidelity F > 0.95
MS gate driven between Sr+ ions
COM motion pre-cooled by Ca+
Shared vibrational mode
cf. work at NIST, ETH

## Slide 11: Cryocooler Vibration Compensation
AOM
0
AOM
AOM
-1
PD
+1
-1
Noise cancelled fiber (~30m)
1m fiber
1m fiber
LO
PID
VCO
fLO = 2 fVCO at lock point
Freq. scanning AOM
MS AOM
-fVCO
+fVCO
Phase compensation of qubit beam through interferometry using auxiliary beam
k
An optical qubit is sensitive to the optical phase of the laser
Wavelength-scale vibrations cause effective dephasing
Aux. beam
Qubit beam
From laser

## Slide 12: Vibration Compensation: Preliminary Results
With phase compensation and cryocooler on, obtain Ramsey coherence times comparable to when cryocooler is off
Investigation in progress: current limit may be due to uncompensated stages, laser linewidth, or B-field fluctuations
Integrated light delivery can potentially make compensation unnecessary

## Slide 13: Introduction and Outline
Dual-Ion-Species Control
  Goal: Use two ion species for scalable transport and readout; work toward high-fidelity gates with photonics
    Two-qubit MS gates (same species, inter-species)
    Two-ion gate in three-ion chain
Anomalous Heating Studies
  Goal: understand and mitigate ion heating to improve speed / fidelity of quantum logic operations
    Ion-electrode distance dependence
    Ex situ milling of Au and Nb traps as a function of T
Integrated Photonics Development
  Goal: develop scalable platform for integrated photonic control over wide wavelength range
    Visible platform: Al2O3/PECVD SiN (low loss, multi-layer, CMOS-compatible)
    Toward High-efficiency photonic I/O

## Slide 14: Ion Trap Material Comparison
Four different metals
  All solvent cleaned
  Au, Pt: No surface oxides
  Nb, Al: Surface oxides
  Nb: S.C. at T < 9K
Taken over several years by different experimenters
General trend is the same
  ~2 orders of magnitude reduction going from RT to 4K
  Some levelling off at low temperature
Al heating rate slightly, but consistently, higher – further study required
Axial 1.3 MHz, ion height 50 um

## Slide 15: Ion Trap Material Comparison
No essential difference between evaporated and electroplated Au
  Notwithstanding very different roughness
All materials seem to have very similar behavior after nominal preparation
5 nm rms
25 nm rms
Data point to contaminating adsorbates on the surface as dominant heating source
Local-chip bake to remove water/solvents (~110 C) did not improve HR

## Slide 16: Distance Dependence
Surface trap, 2 µm niobium on sapphire, 5 zones with ion-electrode distances 29-83 µm
Controlled experiment
  One trap
  No need to break vacuum between measurements
Sedlacek et al., PRA 97, 020302(R) (2018)

## Slide 17: Distance and Frequency Dependence
ftrap=850 kHz
T= 295K
T= 5K
Distance and frequency dependence are the same at high/low T
  Suggests the heating mechanism is the same at 5K and 295 K
  d-4 dependence is not consistent with technical or Johnson noise scalings
64 µm site
T= 295K
T= 5K

## Slide 18: Ex Situ Ion Milling
High energy Ar+ ions
  2 keV, 2.6 uA/cm2 (70 C/m2 for 45 min)
Expose trap briefly to atmosphere during transfer to ion chamber, ~ 1 hour
  No bake required for UHV
Ion milling
Surface contaminants/morphology
Ion gun
Needle Valve
Argon
Trap Chip

## Slide 19: XPS of Nb Traps
Before milling, see only Nb2O5
After milling, get metallic Nb component only
Re-exposure for 30 min leads to 2-component surface

## Slide 20: Ex situ milling of Au, full T dependence
NIST electroplated gold (D. Slichter)

## Slide 21: Change in Heating Temperature Dependence Hypothesis: Two Effects
Lossy dielectrics?
Arrhenius temperature scaling:
T0 = 40 K
Temperature dependence before and after milling
Surface cleaning uncovers a second mechanism
Power-law temperature scaling:
b = 1.5, T0 = 9K
Surface diffusion?

## Slide 22: Ex situ milling of Nb
MIT-LL sputtered niobium

## Slide 23: Material Dependence After Milling
Before milling: Material independence suggests (same) contaminants are dominant—lossy dielectrics?
After milling: New mechanism; material dependence due to exposure of specific surfaces—adatom dipoles? Diffusion?
  Need f, d dependence after milling to distinguish between these

## Slide 24: Frequency/Distance Dependence After Ex Situ Ion Milling
Used variable-height Nb trap to measure f, d dependence
  Pre-milling data from previous measurements
Scalings both appear unchanged
Room-temperature measurements

## Slide 25: Anomalous Heating Status
Understanding surface noise in ion traps
  Distance scaling ~ 1/d4 under several different circumstances
    Unchanged after ex situ milling [also true for freq. (f) scaling]
  Before milling, lossy-dielectric model predictions are closest to data
  Temperature (T) scaling changes after ex situ milling, suggesting a different mechanism in this case
    Adatom-diffusion and fluctuating-dipole models both match T dependence and f or d dependence but not both
  Material dependence emerges after ex situ milling
    Exploring other materials after ex situ milling for more understanding
    E.g., correlate particular metal properties with noise behavior

## Slide 26: Introduction and Outline
Dual-Ion-Species Control
  Goal: Use two ion species for scalable transport and readout; work toward high-fidelity gates with photonics
    Two-qubit MS gates (same species, inter-species)
    Two-ion gate in three-ion chain
Anomalous Heating Studies
  Goal: understand and mitigate ion heating to improve speed / fidelity of quantum logic operations
    Ion-electrode distance dependence
    Ex situ milling of Au and Nb traps as a function of T
Integrated Photonics Development
  Goal: develop scalable platform for integrated photonic control over wide wavelength range
    Visible platform: Al2O3/PECVD SiN (low loss, multi-layer, CMOS-compatible)
    Toward High-efficiency photonic I/O

## Slide 27: Need for Multi-Layer Waveguides
Require 12 different wavelengths for general two-ion species logic
Multiple photonic core materials enable novel device design over large l range
  SiN, Alumina
  Low-loss crossings
  High efficiency I/O gratings
Out-of-Plane:
Loss < 0.001dB/per and reduced cross-talk
In Plane:
Loss ~0.1dB/per
Feeding multiple (~12) wavelengths into each cell in a 2D array with high efficiency is enabled by multi-level photonics
Unit cell concept for scalable ion array

## Slide 28: Measured Loss in LPCVD Si3N4 Waveguides
Loss < 1 dB/cm for 630-1100 nm
Loss in blue rises dramatically
Loss in red and IR appears to be dominated by roughness
  Loss in blue does not follow 1/l4, indicating material loss dominates

## Slide 29: Alumina (Al2O3) Development
Motivation: Low-loss waveguides in the blue to UV
Deposited via ALD (on 8” wafers; CMOS line)
Comparison to SiN:
  nAlumina~ 1.7 (c.f. SiN ~ 2.0)
  Not as confining as SiN
Intrinsic Q: 470,000
l = 405 nm
Ring resonator

## Slide 30: Low-Loss Waveguides From NUV to NIR
Loss < 3 dB/cm from 370 – 1100 nm for SiN + Al2O3 platform

## Slide 31: PECVD SiN Development
Motivation:
  LPCVD SiN is deposited at very high temperature (1100 C)
    Must be deposited before any material incompatible with high T (e.g., metals, Al2O3)
    Precludes continuous metal ground plane for shielding of Si
    Also rules out monolithic integration with CMOS electronics
  PECVD SiN is deposited at low temperature (< 400 C) and does not present these issues
  While LPCVD has shown the lowest loss for red and IR, PECVD loss is sufficient for current ion applications
LPCVD SiN layer stack
PECVD SiN layer stack
Metal
SiN
CMOS in Si
Ground plane with holes
Continuous ground plane

## Slide 32: PECVD SiN Loss Measurement
Developed “UV” PECVD SiN by increasing the ratio of N:Si
  Previous measurements of “standard” PECVD SiN showed very high loss over visible spectrum
PECVD SiN loss comparable to LPCVD from ~600-1100 nm
PECVD SiN loss significantly lower than LPCVD in blue
  But higher loss than Al2O3
Path Forward
PECVD SiN for 600-1100 nm and Al2O3 for blue
Compatible with other integrated control technology and continuous ground plane

## Slide 33: Grating Coupler Measurements
Imaged beam from trap grating coupler designed for 461 nm
  PI beam
Angle: 40 from trap surface
z = 0 um
z = 10 um
z = 20 um
z = 30 um
z = 40 um
z = 50 um
z = 60 um
z = 70 um
z = 80 um
TM light at 461 nm
View: looking down on the chip
z
2w0 = 4 mm
2w0 = 25 mm

## Slide 34: Multi-Wavelength Grating Couplers
Gratings for all Sr+ l’s integrated into ion trap
Grating coupler efficiencies and output beam characteristics measured on bench
  Edge-coupled with PM fiber
Top view
l | Beam waist | Angle of emission | GC Efficiency | Output Intens. (1 mW input) | Compare
422 nm | 2.5 x 10 mm2 | 40 deg | -17 dB (2%) | 0.25 W/cm2 | Isat =.025 W/cm2
460 nm | 2.5 x 10 mm2 | 40 deg | -17 dB (2%) | 2.4 W/cm2 | Isat =.030 W/cm2
674 nm | 2.5 x 9 mm2 | 40 deg | -10 dB (10%) | 23 W/cm2 | Gives tp ~ 8 ms
1092 nm | 3.8 x 9 mm2 | 47 deg | -9 dB (12%) | 11 W/cm2 | Gives Wr ~ 300 MHz

## Slide 35: Input/Output Photonic Coupling: New Grating Coupler Designs
Increasing the efficiency of the input and output coupling
  Currently, we use single-layer, partially-etched, forward-emitting gratings
  Efficiencies are low 2-10%
Solution
  Multilayer SiN gratings for both input and output
    Fully-etched, optical lithography
    Additional layer of nitride breaks symmetry in diffraction grating
    Constructive interference: light preferentially diffracts upwards
  Backward emitting further enhances efficiency
Optical
lithography
Multi-wavelength dual layer grating mask set
405 nm grating
Currently in fabrication

## Slide 36: PECVD SiN/Alumina Multilayer Platform
Key Features:
  Low-loss, high-confinement routing from 400-1100 nm in PECVD SiN and Al2O3
  High-efficiency dual SiN-layer grating couplers for all l
  Multi-layer alumina-to-SiN transitions
FDTD simulations of Al2O3-to-SiN transitions
Al2O3 layer
SiN layer
95% of light transitioned
5 mm
Si
5 mm
SiO2
Via
SiN
Al2O3
Nb trap metal

## Slide 37: Coupling Light from Fibers into Multiple Waveguides
First attempt (6 fibers, 4 for ions): blue output power degraded quickly and drastically
  Commercial packaging house applied epoxy to the fiber-chip interface “bond line” to bond block
    Standard method for fiber attachment (1550 nm)
  Epoxy absorbs and “yellows” when exposed to high intensity blue light (even “UV-transparent” varieties)
    Did not observe yellowing for red and IR
  We tested other epoxies to no avail (mW of blue)
  Bond also broke upon thermal cycling

## Slide 38: Multi-Wavelength Ion Trap: Fiber-to-chip Attachment
Current plan:
  Use viscous, UV-curable epoxy to keep out of bondline
  Use subsequent thermally-cured epoxy (Stycast) to handle cryo/thermal cycling
First demo of this technique showed promising results
  No yellowing for blue light
  Survived one round of cryo-cycling
Need in-house solution to solve this problem efficiently
  Not an industry-solved problem
  Developing capability at LL

## Slide 39: LL Fiber-to-Chip Alignment/Attach Tool
Tool has been designed, assembled, and tested
Fiber-to-chip coupling demonstrated
Currently exploring epoxies best-suited for attachment stability and cryo-cycling
Detector for coupling optimization
Vacuum fiber-block holder for low-strain release
Multi-wavelength ion trap chip
Fiber array block
Red light input coupling
Grating output
6-axis nano-positioner
Electronic epoxy dispensor
Microscope

## Slide 40: Summary
Two-Qubit Gates
  Demonstrated Moelmer-Sorensen gates in Sr+-Sr+, Ca+-Ca+, Sr+-Ca+, Sr+-Ca+-Sr+
  Fidelities 94 - 98.8%
Anomalous Heating Studies
  Measured distance dependence
  Observed change in functional form in T dependence after ex-situ ion milling (both Nb and Au)
Integrated Photonics
  Demonstrated low-loss CMOS-compatible photonics over 370-1100 nm range
  Designed high efficiency grating couplers
  Built fiber-to-chip attachment tool
MIT collaborations: Rajeev Ram and Isaac Chuang groups, RLE
Dave Kharas, Suraj Bramhavar, Colin Bruzewicz, Cheri Sorace-Agaskar, Robert McConnell, Jon Sedlacek, Rich Panock, Jeremy Sage, Jules Stuart, William Loh, John Liddell; Front: Jason Plant, John Chiaverini
(Garrett Simon, Sam Buercklin, Kevin Obenland, Rich Rines, Daniel Kramnik, and Gavin West not shown)

## Slide 41: Next Steps
Electric-field noise
  Adsorbate layer exploration
    Dielectric layers v. hydrocarbons
    Multiple dielectric layers
  Other materials after ex situ milling
Toward improved logic operations using on-chip delivered light
  Robust coupling to trap chip via fibers
  Sr+ ion control with chip-delivered light
  Testing of multi-layer devices with ions: crosstalk, scattering, etc.
  Multi-qubit gates
Dave Kharas, Suraj Bramhavar, Colin Bruzewicz, Cheri Sorace-Agaskar, Robert McConnell, Jon Sedlacek, Rich Panock, Jeremy Sage, Jules Stuart, William Loh, John Liddell; Front: Jason Plant, John Chiaverini
(Garrett Simon, Sam Buercklin, Kevin Obenland, Rich Rines, Daniel Kramnik, and Gavin West not shown)
MIT collaborations: Rajeev Ram and Isaac Chuang groups, RLE